## Slide 1: Dependence of VTH Stability on Gate-Bias Under Reverse-Bias Stress in E-mode GaN MIS-FET
Reporter:
PB21511897 李霄奕
PB21511894 丁书平

## Slide 2: 主要内容
Background
Device
Model
Conclusion

## Slide 3: Background
01

## Slide 4: Background
High power
Electronic vehicle
Sustainable energy
armarium
transportation

## Slide 5: Background
Turn off
Turn on
Strong positive gate bias
Strong negative gate bias
High power switch
  Can be Infinite?
  No!
  VTH Instability

## Slide 6: Device
02

## Slide 7: Device
MIS-FET&MOS-FET
  O=Oxide
  I=insulation
LPCVD&PECVD
High power switch
  GaN
  fully recessed gate structure
  High temp(800C) deposition
  high negative gate bias stress
  VTH Instability

## Slide 8: Device
In-class: Parameter Extraction

## Slide 9: Device
Step-stress VDG=20V:20V:200V
VTH shift<0.14V
Why?
In-class: Transfer Curves

## Slide 10: Device
Why VTH shift?
Trap state density in LPCVD-SiNx
Zener trap in AlGaN-GaN
How to prove it?
After 5 min UV(350 nm) illumination , VTH shift eliminated

## Slide 11: Device
Apply step-stress with VGS=-20V
Aggravated VTH shift

## Slide 12: Device
VTH shift can not be recovered with UV
Trap state?
Ron is independent of VGS
GaN channel?
Gate dielectric!

## Slide 13: Model
hole-induced degradation model
03

## Slide 14: Model
hole-induced degradation model
Strong negative VGD
-> impact ionization
-> enhanced hole flow
-> defect in gate dielectric
-> trap electron
->positive shift of VTH
In-class: Zener Trapping

## Slide 15: Model
hole-induced degradation model
Same temperature: VGS=-20V>0V
0V: temp,
Source-to-drain leakage ,
impact ionization ,
VTH
-20V: temp ,
trap electron ,
VTH

## Slide 16: Model
Switch on
Fill trap state
Filled
In-class: Trap State

## Slide 17: Conclusion
04

## Slide 18: Conclusion
VTH instability found in long time strong negative VGS
A hole-induced degradation model
Choose a suitable VGS to obtain stable VTH in high-power switching

## Slide 19: Thank you！